Laszlo Corporation

3 Mannington Ct

St. Peters, Missouri 63376

(636) 447-1312

(636) 614-2599 FAX

CAUSTIC SODA

(FLAKES 98%)

PRODUCTS NAME: CAUSTIC SODA  (FLAKES 98%)

CAS RN.: 1310-73-2

SPECIFICATION:

| ITEMS | SPECIFICATION | RESULTS |
| --- | --- | --- |
| NaOH (%min) | 98% | 98.12 |
| Na2CO3 (%max) | 0.9 | 0.78 |
| NaCl (%max) | 0.05 | 0.004 |
| Fe2O3 (%max) | 0.0005 | 0.00035 |

PACKAGE: PACK IN 25KG PLASTIC BAG, 25MT/FCL