Laszlo Corporation

3 Mannington Ct

St. Peters, Missouri 63376

(636) 447-1312

(636) 614-2599 FAX

TCPP SPECIFICATION

.Synonyms: TCPP, tris(2-chloroisopropyl) phosphate, Fyrol PCF
2.Molecular Formula: C9H18CL3O4P
3.Molecular Weight: 327.56
4.CAS No.: 13674-84-5
5.Quality of product:

| Items | Index |
| --- | --- |
| Appearance | Colorless or light-yellow transparent liquid |
| Color(APHA) | 50Max |
| Acidity(mgKOH/g) | 0.10Max |
| Water Content | 0.10%max |
| Viscosity(25℃) | 67±2CPS |
| Flash Point ℃ | 210 |
| Phosphorus Content | 9.4% |
| Refractive Index | 1.4630-1.4645 |
| Specific Gravity | 1.280-1.290 |

It is colorless transparent oily liquid , Specific gravity(20°C/20°C)1.29, refractive index is N20D1.460-1.466, Flash point(open)220°C, Cl 32.5%, P 9.46%, viscosity :85mps20°C ;soluble in ethanol and chloroform,insoluble in aliphatic hydrocarbon, water solubility is less than 1%..

It is mainly used as f soft or hard polyurethane foam, epoxy resin polystyrene, acrylic acid, cellulose acetate, ethyl cellulose paint, phenolic plastics, polyvinyl acetate and foam leak sealing agent. It has good heat conductivity and hydrolysis stabilizer, especially suitable for ASTME84( grade). Its products have low viscosity in low temperature when it is used in polyurethane foam , unsaturated polyester and phenolic plastic.